Regulation (EU) No 528/2012 concerning the making available on the market and use of biocidal products

PRODUCT ASSESSMENT REPORT
OF A BIOCIDAL PRODUCT FOR RENEWAL

OF A NATIONAL AUTHORISATION

Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat

Product type 8 (Wood preservatives)

Active substances:

Disodium tetraborate

Boric acid

Case Number in R4BP: BC-VM033649-12

Evaluating Competent Authority: Poland

Date: March 2019

Contents

1	CONCLUSION	3

2	General information about the product application	5

2.1	Applicant	5

2.1.1	Person authorised for communication on behalf of the applicant	5

2.2	Information about the product application	6

2.3	Information about the biocidal product	6

2.3.1	General information	6

2.3.2	Information on the intended use	7

2.3.3	Information on active substances	8

2.3.4	Information on the substance(s) of concern	9

2.4	Documentation	10

2.4.1	Data submitted in relation to product application	10

2.4.2	Access to documentation	10

3	Summary of the product assessment	10

3.1	Identity related issues	10

3.2	Classification, labelling and packaging	10

3.2.1	Harmonised classification of the biocidal product	10

3.2.2	Labelling of the biocidal product	10

3.2.3	Packaging of the biocidal product	12

3.3	Physical-chemical properties and analytical methods	13

3.3.1	Physical-chemical properties	13

3.3.2	Analytical methods	16

3.4	Risk assessment for physical-chemical properties	16

3.5	Effectiveness against target organisms	17

3.5.1	Function	17

3.5.2	Field of usage	17

3.5.3	Effect of target organisms	18

3.5.3.1	Wood destroying basidiomycetes	18

3.5.3.2	Wood boring beetles	21

3.5.4	Discussion	22

3.5.4.1	Wood destroying basidiomycetes	22

3.5.4.2	Wood boring beetles	24

3.5.5	Conclusion	25

3.6	Exposure assessment	25

3.6.1	Description of the intended use	25

3.6.2	Assessment of exposure to humans and the environment	25

3.7	Risk assessment for human health	26

3.7.1	Hazard potential	26

3.7.1.1	Toxicology of the active substance	26

3.7.1.2	Toxicology of the substance(s) of concern	27

3.7.1.3	Toxicology of the biocidal product	27

3.7.2	Exposure	33

3.7.2.1	Exposure of industrial and professional users	34

3.7.2.1.1	Vacuum pressure	34

3.7.2.1.2	Dipping	37

3.7.2.1.3	Painting/brushing:	39

3.7.2.2	Non-professional exposure	40

3.7.2.3	Indirect exposure as a result of use of the active substance in biocidal product	41

3.7.2.3.1	Exposure during cutting and sanding by professionals	41

3.7.2.3.2	Exposure during cutting and sanding by non-professionals	42

3.7.2.3.3	Exposure of a child playing on playground structure outdoors	43

3.7.3	Risk Characterisation	46

3.7.3.1	Risk for industrial and professional users	46

3.7.3.2	Indirect exposure as a result of use of the active substance in biocidal product	50

3.8	Risk assessment for the environment	50

3.8.1	Fate and distribution in the environment	51

3.8.2	Emission to environmental compartments	51

3.8.3	Environmental risk assessment	53

3.8.3.1	Aquatic compartment	53

3.8.3.1.1	Surface water and sediment	53

3.8.3.1.2	Sewage treatment plant	54

3.8.3.2	Atmosphere	54

3.8.3.3	Terrestrial compartment	54

3.8.3.4	Groundwater	54

3.8.4	Non compartment specific effects relevant to the food chain  (secondary poisoning)	55

3.8.5	Comparative assessment	55

3.9	Measures to protect man, animals and the environment	57

4	Proposal for decision	60

Annex 1:	List of studies reviewed	61

Annex 2:	Analytical methods residues – active substance	67

Annex 3:	Toxicology and metabolism –active substance	68

Annex 4:	Toxicology – biocidal product	69

Annex 5:	Safety for professional operators	71

Annex 6:	Safety for non-professional operators and the general public	72

Annex 7:	Residue behaviour	73

Annex 8:	Confidential information – ONLY FOR RMS INFORMATION, NOT FOR APPLICANT	74

# CONCLUSION

The Polish CA has processed an application for renewal  of the authorisation of the biocidal product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat which contains the active substances Boric acid (15% w/w) and Disodium tetraborate (5% w/w).

The product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is a powder to prepare liquid solution.

The product has been classified according to the 1st (corr) ATP of Regulation (EC) No1272/2008 (Commission Regulation (EU) 2018/669 of 16 April 2018).

The biocidal product has been documented as efficient against wood destroying basidiomycetes, wood boring beetles (Hylotrupes bajulus).

The long-term stability study showed an acceptable degradation of the active substances, thus a claim for 2 years shelf-life can be accepted in HDPE containers.

The biocidal product is intended for use by professional and industrial users, recommended methods of application are painting/brushing, dipping and vacuum pressure.

The assessment presented in the Product Assessment Report for the first authorisation showed adverse health effects for unprotected industrial and professional users due to combined dermal and respiratory exposure in case of vacuum pressure impregnation, manual and automated dipping processes. As a consequence, protective clothing (gloves, coveralls, and foot protection) and respiratory protection are necessary to reduce the exposure.

No emission scenarios are available for UC1 and UC2 use classes of wood, thus the potential risk from treated wood to the outer environment is considered negligible. However, in the case of application and storage of treated wood prior to shipment, the following specific provision was included “In particular, labels and/or safety-data sheets of products authorised for industrial use shall indicate that freshly treated timber must be stored after treatment under shelter and/or on impermeable hard standing to prevent direct losses to soil or water and that any losses must be collected for reuse or disposal”.

Comparative assessment

As a consequence of the new harmonised classification, the active substances Boric acid (15% w/w) and Disodium tetraborate (3% w/w) meet the criteria for exclusion according to Article 5(1) BPR as well as for substitution according to Article 10(1)(a) BPR. Therefore, in line with Article 23(1) BPR a comparative assessment for the product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat has been conducted. The outcome of the comparative assessment was not sufficiently conclusive to state that the criteria of Article 23(3) of EU Regulation 528/2012 are met.

Overall conclusion

No new data were provided on Wood Protector przeciwogniowy impregnat do drewna FIRESTOP. Therefore, the assessment of the biocidal product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat and the first authorisation remain valid. However, the terms and conditions of authorisation have been adapted, where necessary, taking into account the points mentioned above.

The biocidal product is authorised according to Article 31(2) BPR and renewed for 5 years according to Article 23(6) BPR.

Chronology:

- First authorisation – 5 March 2014

- Shortening the valid period after authorisation granting – 30 August 2017

- Renewal authorisation - March 2019

The current PAR is based on PAR of first authorisation. The text marked in grey refers to the parts introduced or changed during renewal assessment (NA-RNL).

# General information about the product application

## Applicant

| Company Name: | Dekspol P.P.H. Iwona Oleszak |
| --- | --- |
| Address: | ul. Terespolska 13 |
| City: | Poznań |
| Postal Code: | 61-047 |
| Country: | Poland |
| Telephone: | +48 61 640 00 04 |
| Fax: | +48 61 640 00 09 |
| E-mail address: | k.siekierska@dekspol.pl |

### Person authorised for communication on behalf of the applicant

| Name: | Kinga Siekierska |
| --- | --- |
| Function: | Quality Assurance Manager |
| Address: | Garaszewo 44c Street |
| City: | Poznań |
| Postal Code: | 61-323 |
| Country: | Poland |
| Telephone: | +48 604 597 840 |
| Fax: | +48 61 640 00 09 |
| E-mail address: | k.siekierska@dekspol.pl |

## Information about the product application

| Application received: | 30 August 2011 |
| --- | --- |
| Application reported complete: | 17 April 2012 |
| Type of application: | National authorisation |
| Further information: | No |

## Information about the biocidal product

### General information

| Trade name: | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat |
| --- | --- |
| Manufacturer’s development code number(s), if appropriate: | ( |
| Product type: | 8 (wood preservatives) |
| Composition of the product (identity and content of active substance(s) and substances of concern; full composition see confidential annex): | Boric acid 15.0% Disodium tetraborate 5.0% |
| Formulation type: | Powder |
| Ready to use product (yes/no): | No |
| Is the product the very same (identity and content) to another product already authorised under the regime of Regulation (EU) No 528/2012 (yes/no); If yes: authorisation/registration no. and product name: or Has the product the same identity and composition like the product evaluated in connection with the approval in accordance with Regulation (EU) No 528/2012 (yes/no): | No |

### Information on the intended use

| Overall use pattern (manner and area of use): | Use classes: UC 1 (wood or wood-based product under cover and fully protected from the weather, not exposed to wetting) UC 2 (wood or wood-based product under cover and fully protected from the weather but where high environmental humidity can lead to occasional but not persistent wetting) Application method: Painting/brushing Dipping Vacuum pressure |
| --- | --- |
| Target organisms: | Wood destroying Basidiomycetes: Coniophora puteana, Gloeophyllum trabeum, Poria placenta Wood boring beetle: Hylotrupes bajulus, larvae |
| Category of users: | Professional Industrial |
| Directions for use including minimum and maximum application rates, application rates per time unit (e.g. number of treatments per day), typical size of application area: | superficial treatment 500 g/m2 of 20% working solution (100 g/m2 of concentrate) penetrating treatment 25 kg/m3 of 20% working solution (5 kg/m3 of concentrate). These doses are effective for prevention of against the wood rooting fungi and wood boring insects together |
| Potential for release into the environment (yes/no): | Yes |
| Potential for contamination of food/ feeding stuff (yes/no) | No |
| Proposed Label: | - |
| Use Restrictions: | Please referee to section 3.9 |

### Information on active substances

| Active substance chemical name: | Boric acid | Disodium tetraborate |
| --- | --- | --- |
| CAS No: | 1043-35-3 | 1330–43–4 |
| EC No: | 233-139-2 | 215–540–4 |
| Purity (minimum, g/kg or g/l): | > 990 g/kg | > 990 g/kg |
| Inclusion directive: | 2009/94/EC | 2009/91/EC |
| Date of inclusion: | 01.09.2011 | 01.09.2011 |
| Is the active substance equivalent to the active substance in accordance with Regulation (EU) No 528/2012 (yes/no): | Yes | Yes |

Manufacturer of active substance used in the biocidal product

| Company Name: | US Borax Inc | ETI MADEN ISLETMELERI |
| --- | --- | --- |
| Address: | 14486 Borax Road | Korkutreis Mah., Cihan Sok. No:2 |
| City: | Boron, CA | Sıhhiye Çankaya, Ankara |
| Postal Code: | 93516-2000 | 06430 |
| Country: | USA | Turkey |
| Telephone: | + 1 760 762 7000 | - |
| Fax: | - | - |
| E-mail address: | - | - |

| Active substance | Boric acid |
| --- | --- |
| Name of manufacturer 1 | U.S. Borax Inc. Boron Operations |
| Address of manufacturer 1 | 14486, Borax Road, California 93516-2000, Boron, USA |
| Location of manufacturing sites 1 | 14486, Borax Road, California 93516-2000, Boron, USA |
| Name of manufacturer 2 | ETI MADEN ISLETMELERI |
| Address of manufacturer 2 | Korkutreis Mah., Cihan Sok. No:2, Sihhiye Cankaya 06430, Ankara, Turkey |
| Location of manufacturing sites 2.1 | Eti maden isletmeleri g.m. Bandirma bor ve asit fab. Islt. Mudurlugu, Bandrima 10200, Balikesir, Turkey |
| Location of manufacturing sites 2.2 | Eti maden islemeleri g.m. Emet kolemanit Islt. Mudurlugu, Emet 43700, Kutahya, Turkey |

| Active substance | Disodium tetraborate |
| --- | --- |
| Name of manufacturer 1 | U.S. Borax Inc. Boron Operations |
| Address of manufacturer 1 | 14486, Borax Road, California 93516-2000, Boron, USA |
| Location of manufacturing sites 1 | 14486, Borax Road, California 93516-2000, Boron, USA |
| Name of manufacturer 2 | ETI MADEN ISLETMELERI |
| Address of manufacturer 2 | Korkutreis Mah., Cihan Sok. No:2, Sihhiye Cankaya 06430, Ankara, Turkey |
| Location of manufacturing sites 2.1 | Eti maden isletmeleri g.m. Bandirma bor ve asit fab. Islt. Mudurlugu, Bandrima 10200, Balikesir, Turkey |
| Location of manufacturing sites 2.2 | Eti maden islemeleri g.m. Emet kolemanit Islt. Mudurlugu, Emet 43700, Kutahya, Turkey |

### Information on the substance(s) of concern

| Substance chemical name | benzyl-C12-14-alkyldimethyl, chlorides |
| --- | --- |
| CAS No: | 85409-22-9 |
| EC No : | 287-089-1 |
| Purity (minimum, g/kg or g/l): | ≥99% |
| Typical concentration (minimum and maximum, g/kg, or g/l): | 0.66% wag |
| Relevant toxicological/ecotoxicological information: | H302, H314, H400 P273, P280, P305 + P351 + P338, P 310 |
| Original ingredient (trade name): | Barquat MS-100 |

## Documentation

### Data submitted in relation to product application

Please see to Annex 2.

### Access to documentation

Dekspol P.P.H. Iwona Oleszak has letter of access (dated on 18 August 2011) to data held by European Borates Association A.I.S.B.L. which was used to supports the Annex I listing of the active substances boric acid and disodium tetraborate according to Directive 98/8/EC.

# Summary of the product assessment

## Identity related issues

The biocidal product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat contains two active substances – boric acid (15%) (purity > 990 g/kg) and disodium tetraborate (5%) (purity > 990 g/kg).

The source of active substances used in the biocidal product is identical to the active substances that is listed in Annex I of 98/8/EC.

## Classification, labelling and packaging

### Harmonised classification of the biocidal product

T- Toxic

R60, R61

### Labelling of the biocidal product

The current Classification of Boric acid under Dir 67/548/EEC is:

T- Toxic

R60, R61

The current Classification of Boric acid under EC 1272/2008 is:

Repr. 1B, H360FD

The current Classification of Disodium tetraborate under Dir 67/548/EEC is:

T- Toxic

R60, R61

The current Classification of Disodium tetraborate under EC 1272/2008 is:

Repr. 1B, H360FD

Classification and labelling of the product under Dir 67/548/EEC is:

R-phrases

T: R60, R61

S-phrases

S2 – Keep out of the reach of children.

S36/39 – Wear suitable protective clothing and eye/face protection

S45 – In case of accident or if you feel unwell, seek medical advice immediately (show the label whenever possible).

S53 – Avoid exposure – obtain special instructions before use.

Classification and labelling of the product under EC 1272/2008 is:

Hazard statements:

Repr. 1B, H360FD

Precautionary statements:

P102 – Keep out of the reach of children.

P103 – Read label before use.

P280 – Wear suitable protective clothing and eye/face protection.

P308+P313 – IF exposed or concerned: Get medical advice/attention.

Harmonised classification and labelling of the biocidal product according to the Regulation (EC) 1272/2008

| Classification |
| --- |
| Hazard category | Repr. 1B |
| Hazard statement | H360FD May damage fertility or the unborn child. |
| Signal words | Danger |
| Hazard statements | H360FD May damage fertility or the unborn child. |
| Precautionary statements | P102 Keep out of the reach of children. P103 – Read label before use. P280 – Wear protective gloves/protective clothing/eye protection/face protection. P308+P313 – IF exposed or concerned: Get medical advice/attention. P501 Dispose of contents/container to … |
| Note |  |

### Packaging of the biocidal product

The packaging details for the biocidal product, Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, are outlined below for professional and industrial users.

| Packing type | Pack sizes for professional and industrial users |
| --- | --- |
| Buckets made of HDPE | 1 kg |
| Buckets made of HDPE | 5 kg |
| Buckets made of HDPE | 10 kg |
| Buckets made of HDPE | 20 kg |
| Bags made of polyethylene | 10 kg |
| Bags made of polyethylene | 20 kg |

## Physical-chemical properties and analytical methods

The product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is a powder, which is used to prepare the working solution (20% water solution) of biocidal product.

Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is whitish powder with characteristic odour with no oxidizing nor explosive properties. It is also not fulfilling a criterion for highly flammable and is not self igniting up to 400°C. Tap density of the product is equal to 0.77 kg/m3. Water suspension of the product gives slightly-acetic pH (1%, pH = 6.58 to 6.57 – after storage stability test). Product is highly soluble in water. Due to test results, creation of persistent foam is expected to occur.

Taking into consideration results from the accelerated storage stability test and also stability of technical characteristics, the shelf life of the product is considered acceptable up to two years in ambient conditions.

The colorimetric method according to method described in AOAC. vol. 10 number 31.049, 31.050 and 31.051 with rules of GLP and SANCO/3030/99. rev.4 guide is acceptable for determination of the active substance content in the product.

### Physical-chemical properties

Physical-chemical properties of the active substance:

The letter of access from European Borates Association A.I.S.B.L in short “EBA”, granted to Dekspol P.P.H. Iwona Oleszak, has been submitted for the active substance therefore no additional information for this point is needed.

Physical-chemical properties of the biocidal product:

|  | Method | Purity/ Specification | Results | Reference |
| --- | --- | --- | --- | --- |
| Physical state and nature | Polish Pharmacopoeia VI Edition (2002) and according to EPA Product Properties Test Guideline OPPTS 830.6302 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, partia nr (lot No.) DP.10.05.11.P 94. | Solid particles | EMC Nr 373800019, BF-25/11 |
| Colour | Farmakopea Polska, wyd. VI (2002) and according to EPA Product Properties Test Guideline OPPTS 830.6303 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, partia nr (lot No.) DP.10.05.11.P 94. | whitish | EMC 373800019 study code: BF-25/11 |
| Odour | Farmakopea Polska, wyd. VI (2002) and according to EPA Product Properties Test Guidelines OPPTS 830.6304 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, partia nr (lot No.) DP.10.05.11.P 94. | characteristic | EMC Nr 373800019, BF-25/11 |
| Explosive properties | n.a. | n.a. | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat does not possess explosive properties | n.a. |
| Oxidizing properties | n.a. | n.a. | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat does not possess oxidizing properties | n.a. |
| Flash point | n.a. | n.a. | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is not highly flammable | n.a. |
| Autoflammability | n.a. | n.a. | The self-ignition of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat did not occur up to 400 °C | n.a. |
| Other indications of flammability | n.a. | n.a. | n.a. | n.a. |
| Acidity / Alkalinity | CIPAC MT 75 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, partia nr (lot No.) DP.10.05.11.P 94. | pH of 1% water suspension is 6.58 before and 6.57 after accelerated storage stability test | EMC 373800019 study code: BF-25/11 |
| Relative density / bulk density | CIPAC MT 186 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, partia nr (lot No.) DP.10.05.11.P 94. | Tap density is 0.77 g/l | EMC 373800019 study code: BF-25/11 |
| Storage stability – stability and shelf life | CIPAC MT 46 (2 weeks 54 °C) | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, partia nr (lot No.) DP.10.05.11.P 94. | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is stable for two weeks in 54 °C | EMC 373800019 study code: BF-25/11 |
| Effects of temperature | n.a. | n.a. | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is stable for two weeks in 54 °C | n.a. |
| Reactivity towards container material | CIPAC MT 46 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, partia nr (lot No.) DP.10.05.11.P 94. | the weight, colour and shape of container as well as physical-chemical properties of product did not change during storage stability test | EMC 373800019 study code: BF-25/11 |
| Technical characteristics in dependence of the formulation type Wettability |  | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, partia nr (lot No.) DP.10.05.11.P 94. | 0 sec, the powder is wettable immediately | EMC 373800019 study code: BF-25/11 |
| Persistence of foaming | CIPAC MT 47 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat partia nr (lot No.) DP.10.05.11.P 94. | After 12 min. 8 ml of foam | EMC 373800019 study code: BF-25/11 |
| Compability with other products | n.a. | n.a. | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat will not be used with other products (expecially biocidal products) | n.a. |
| Surface tension | n.a. | n.a. | n.a. | n.a. |
| Viscosity | n.a. | n.a. | n.a. | n.a. |
| Particle size distribution | CIPAC MT 59 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat partia nr (lot No.) DP.10.05.11.P 94. | 22.49% ≥ 1400 µm 1000 µm ≤ 10.23 % < 1400 µm 710 µm ≤ 15.48 % < 1000 µm 500 µm ≤ 29.06 % < 710 µm 250 µm ≤ 22.03 % < 500 µm 125 µm ≤ 0.72 % < 250 µm 63 µm ≤ 0 % < 125 µm | EMC 373800019 study code: BF-25/11 |

### Analytical methods

|  | Principle of method |
| --- | --- |
| Technical active substance as manufactured: | ( |
| Impurities in technical active substance: | ( |
| Active substance in the formulation: | Specific analytical method with validation data was established for determination of content of the active substance in the product. The colorimetric method according to method described in AOAC. vol. 10 number 31.049, 31.050 and 31.051 with rules of GLP and SANCO/3030/99. rev.4 guide. In this method the total content of borates was determined by spectrophotometer in UV in water solutions containing colour complex - product of reaction of borates with curcumin in acidic solution. |

## Risk assessment for physical-chemical properties

Based on the physical-chemical data submitted for Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat Polish Competent Authority can conclude that there are no additional, specific physical-chemical risks for the product. The product has no explosive nor oxidizing properties. The product is not highly flammable and there are not autoflammability indications up to 400°C. Due to test results, creation of persistent foam is expected to occur. Technical properties characteristics of the product are done before and after accelerated storage stability test. No additional risks are found based on technical characteristics of a product (e.g. no potential inhalation danger since particles size < 125 µm are present as trace (0.72 % < 250 µm).

Taking into consideration results from the accelerated storage stability test, the shelf life of the product is considered acceptable up to two years in ambient conditions.

## Effectiveness against target organisms

### Function

Product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP KONCENTART is concentrated wood preservative to preserve against wood destroying basidiomycetes and wood boring beetles. The biocidal product concentrate is diluted with water to a 20% working solution. Certain efficacy data have been generated for the product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat.

### Field of usage

The product contains 15% boric acid and 5% disodium tetraborate. The final concentration of active substances in working solution is 3% of boric acid 1% of disodium tetraborate. The product is intended to be used on wood above-ground in use classes 1 and 2.

According to label claims the product is efficient against wood destroying basidiomycetes and wood boring beetles.

The product is applied by professional and industrial users by superficial treatment (painting/brushing and dipping) to give an application rate of:

- 40 g product m2 (200 g/m2 of 20% solution of concentrate) in 2 or more coats against wood destroying basidiomycetes (6 g boric acid m2 and 2 g disodium tetraborate m2)

- 100 g product m2 (500 g/m2 of 20% solution of concentrate) in 4 or more coats against wood boring beetles and wood destroying basidiomycetes (15 g boric acid m2 and 5 g disodium tetraborate m2)

and by penetrating process (by vacuum pressure):

- 2.5 kg product m3 (12.5 kg/m3 of 20% solution of concentrate) to protect against the attack of wood destroying basidiomycetes (0.38 kg boric acid m3 and 0.13 kg/disodium tetraborate m3),

- 5 kg product m3 (25 kg/m3 of 20% solution of concentrate) is effective for prevention against the attack of beetle and wood destroying basidiomycetes (0.75 kg boric acid/m3 and 0.25 kg disodium tetraborate/m3).

### Effect of target organisms

#### Wood destroying basidiomycetes

Study 1

In study conducted according to test standard PN-ENV 839:2008, efficacy of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP was tested against wood destroying basidiomycetes.

The blocs used in the test were artificially aged according to PN-EN 73:1993.

Table 2.1Percentage of mass loss of virulence specimens

| Test fungus/wood species | Mass loss | Average loss [%] | Requested minimal value according to PN-ENV 839 [%] |
| --- | --- | --- | --- |
|  | [g] | [%] |  |  |
| Coniophora puteana BAM Ebw. 15 Scotch pine sapwood | 3.67 3.30 2.57 2.86 3.50 3.74 | 42.77 39.90 29.61 34.05 40.89 47.10 | 39.1 | 20.0 |
| Gloeophyllum trabeum BAM Ebw. 109 Scotch pine sapwood | 1.85 2.22 2.42 2.73 2.91 2.07 | 22.26 27.07 28.57 31.89 33.45 25.37 | 28.1 | 20.0 |
| Poria placenta FPRL 280 Scotch pine sapwood | 1.92 2.21 1.72 2.80 1.80 2.11 | 21.69 27.18 21.55 31.67 21.95 25.86 | 25.0 | 20.0 |

Toxic threshold concentrations in superficial application were determined as follows:

- Coniophora puteana  200 g/m2 of ready for use product (40 g/m2 of concentrate) assuming wood density 0.51 g/cm3

- Gloeophyllum trabeum 200 g/m2 of ready for use product (40 g/m2 of concentrate) assuming wood density 0.51 g/cm3

- Poria placenta 200 g/m2 of ready for use product (40 g/m2 of concentrate) assuming wood density 0.51 g/cm3

Biological reference value against basidiomycetes after evaporation is 200 g/m2.

Study 2

In a second study conducted according to a standard PN-EN 113:2000/A1:2005, efficacy  of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP was tested against wood destroying basidiomycetes.

In this study serial dilutions of product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat was tested.

The blocs used in the test were artificially aged according to PN-EN 73:1993.

Table 2.2 Toxic values for Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat (arithmetic means of 6 replicates).

| Test fungus/wood species | Concentration of preservative solution [% (w/w)] | Preservative absorption [kg/m3] | Average of the adjusted mass loss of the highest concentration without protective effectiveness [%] |
| --- | --- | --- | --- |
| Coniophora puteana BAM Ebw. 15 Scotch pine sapwood | 0.25 – 0.40 | 1.49 – 2.42 | 23.7 |
| Gloeophyllum trabeum BAM Ebw. 109 Scotch pine sapwood | 0.25 – 0.40 | 1.51 – 2.43 | 6.2 |
| Poria placenta FPRL 280 Scotch pine sapwood | 0.25 – 0.40 | 1.53 – 2.45 | 6.4 |

Table 2.3 Percentage of mass loss of virulence specimens

| Test fungus/wood species | Mass loss [%] | Average loss [%] | Requested minimal value according to PN-EN 113:2000 [%] |
| --- | --- | --- | --- |
| Coniophora puteana BAM Ebw. 15 Scotch pine sapwood | 34.58 44.89 37.16 43.56 33.49 39.09 | 38.8 | 20.0 |
| Gloeophyllum trabeum BAM Ebw. 109 Scotch pine sapwood | 35.26 31.61 32.07 25.06 27.07 32.16 | 30.5 | 20.0 |
| Poria placenta FPRL 280 Scotch pine sapwood | 24.26 23.05 20.81 20.99 25.65 26.67 | 23.6 | 20.0 |

The test results showed that the b.r.v (biological reference value) were 2.42 kg of product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP against C. puteana, 2.42 kg/m3 against G. trabeum and 2.43 kg/m3 against P. placenta

#### Wood boring beetles

Study 1

In this study conducted according to a test standard PN-EN 46-1:2009 Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat was tested for efficacy against wood boring beetles (recently hatched larvae of Hylotrupes bajulus).

The blocs used in the test were artificially aged according to PN-EN 73:1993.

As 90 – 100% of the larvae exposed to the untreated control test specimens and of those exposed to control test specimens treated with the solvent survived, therefore the test is valid.

Table 2.4 Summary results for Wood Protector przeciwogniowy impregnat do drewna FIRESTOP (6 replicates)

| Concentration tested [% (w/w)] | Solution retention [g/m2] | Number of larvae | Number of larvae not recovered [n] |
| --- | --- | --- | --- |
|  |  | Dead | Alive [n] |  |
|  |  | Not gnawed [n] | Gnawed [n] |  |  |
| 20 | 498.4 | 6 | 4 | 0 | 0 |
|  | 500.0 | 9 | 1 | 0 | 0 |
|  | 498.4 | 4 | 6 | 0 | 0 |
|  | 500.0 | 7 | 3 | 0 | 0 |
|  | 499.2 | 6 | 4 | 0 | 0 |
|  | 499.2 | 8 | 2 | 0 | 0 |

The test results indicated that, following treatment at an application rate of 500 g/m2 of ready to use product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat all larvae are dead.

Study 2

In this study conducted according to a test standard EN 47:2005, Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat was tested for efficacy against wood boring beetles (recently hatched larvae of Hylotrupes bajulus).

The blocs used in the test were artificially aged according to PN-EN 73:1993.

Table 2.5 Determination of the toxic values against Hylitrupes bajulus (L.) according to EN 47

| Concentration of product tested [% m/m] | Retention of wood preservative Mean [kg/m3] | Number of larvae |
| --- | --- | --- |
|  |  | Dead | Alive [n] | Not discovered [n] |
|  |  | Not gnawed [n] | Gnawed [n] |  |  |
| Examination after 4 weeks |
| 2.78 | 20.5 | 1 | 29 | 0 | 0 |
| 2.08 | 15.3 | 2 | 28 | 0 | 0 |
| 1.39 | 10.2 | 0 | 0 | 1 a) | 0 |
| Examination after 12 weeks |
| 1.39 | 10.2 | 2 b) | 27 b) | 0 | 0 |
| 0.97 | 7.1 | 0 | 30 | 0 | 0 |
| 0.69 | 5.1 | 0 | 30 | 0 | 0 |
| 0.00 (water) | 0.0 | 0 | 0 | 29 | 1 |
| control | - | 1 | 0 | 29 | 0 |

- No further splitting up after 4 weeks of testing

- Referring to the remaining test blocks after 12 weeks

Study results showed that toxic values after 12 weeks test duration are < 5.1 kg/m3, product concentration 0.69 %

### Discussion

#### Wood destroying basidiomycetes

The study conducted according to CEN/TS 839:2008 was carried out at rate 200 g/m2 and 250 g/m2 of 20% solution of product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat.

The study showed that product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is efficient in rate 200 g/m2 of 20% working solution.

The superficial application rate against wood destroying basidiomycetes for the product is 200 g/m2 of 20% working solution (6 g boric acid m2 and 2 g disodium tetraborate m2).

Dipping application method used in the test is the superficial treatment. Brushing is also a superficial method and in the Polish Competent Authority view, the results support label claims for all requested superficial application methods.

The study conducted according to CEN/TS 839:2008 was carried out at rate 200 g/m2 and 250 g/m2 of ready to use product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP.

According to European standard EN 599-1, the critical value (c.v.) is the highest b.r.v from all of the biological tests carried out on the product. Therefore the c.v. derived in the test study conducted according to PN-EN 113:2000 on product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is 2.43 kg/m3 witch correspond with 12.15 kg/m3 of 20% working solution (0.37 kg boric acid/m3 and 0.11 kg disodium tetraborate/m3).

The application rate against wood destroying basidiomycetes is 2.5 kg product/m3, 12.5 kg/m3 of 20% working solution of concentrate (0.38 kg boric acid m3 and 0.13 kg disodium tetraborate/m3)/

Therefore, the data supports declared by Applicant application rate for penetrating treatment against wood destroying basidiomycetes with Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat.

For the above reasons Polish Competent Authority considers the data to be acceptable in support of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat.

#### Wood boring beetles

The EN 46-1:2009 study demonstrated the efficacy of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat as a preventive wood preservative against wood boring beetles at a superficial application rate of 100 g product/m2 – 500 g/m2 of 20% working solution (15 g boric acid/m2 and 5 g disodium tetraborate/m2).

The Applicant has indicated that the superficial application rate of the product against wood boring beetles is 500 g product/m2 (15 g boric acid/m2 and 5 g disodium tetraborate/m2). Therefore the results support proposed application rate of the product.

The brush application method used in the test is the superficial treatment. Dipping is also a superficial method and in the Polish Competent Authority view, the results support label claims for all requested superficial application methods.

The EN 47:2005 study demonstrated the efficacy of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat as a preventive wood preservative against wood boring beetles at a penetrative application rate of >5.1 kg product/m3 – 25.5 kg/m3 of 20% working solution (0.76 kg boric acid/m3 and 0.26 kg disodium tetraborate/m3).

The Applicant has indicated that the penetrative application rate of the product against wood boring beetles is 5 kg of product/m3 (0.75 kg boric acid/m3 and 0.25 kg disodium tetraborate/m3). Although this is lower than the rate shown in the test to be effective, the difference is minimal. The Polish Competent Authority does not consider this difference to be an issue, and is satisfied that the results support declared by Applicant application rates for penetrative treatment with Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. Therefore the results support proposed application rate of the product.

The Applicant has declared that the product is intended for use in 1 and 2-wood use classes. On the basis on TNsG on Product Authorisation, Appendices to Chapter 7, Product Type 8, Section 2.2.1, the submitted data meet the required criteria for use classes 1 and 2.

For the above reasons Polish Competent Authority considers the data to be acceptable in support of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat.

### Conclusion

Sufficient data confirming efficacy in declared field of use have been generated on the product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat.

## Exposure assessment

### Description of the intended use

Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is a wood preservative for preventive use against wood destroying basidiomycetes and wood boring beetles. Biocidal product is intended to use in use class 1 (UC1 – wood or wood-based product under cover and fully protected from the weather, not exposed to wetting) and in use class 2 (UC2 – wood or wood-based product under cover and fully protected from the weather but where high environmental humidity can lead to occasional but not persistent wetting).

The biocidal product is intended for professional and industrial users, recommended method of application is painting/brushing, dipping and vacuum pressure.

The product contains 15% w/w of boric acid and 5% w/w disodium tetraborate and it is used to prepare the product ‘ready to use’ (20% water solution of the concentrate) which contains 3% w/w of boric acid and 1% w/w of disodium tetraborate. Both substances are relevant for the risk assessment of the biocidal product. The toxic effects of them are similar and in both cases due to the content of boron. Therefore, in the exposure calculations the active substances will be expressed as B (boron) equivalents; the conversion factors for boric acid and disodium tetraborate into equivalent doses of boron are 0.175 and 0.215, respectively.

### Assessment of exposure to humans and the environment

The biocidal product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat contain two active substance: boric acid and disodium tetraborate and one substance of concern – quaternary ammonium compounds, benzyl-C12-14-alkyldimethyl, chlorides (CAS 85409-22-9), trade name Barquat MS 100, classified and labelled under CLP regulation 1272/2008. The Barquat MS 100 concentration in the product is very low (0.66%) and does not affect on overall classification of product. Please see Document IIIB6.5 for details.

New exposure studies have not been submitted and the risk assessment was performed based on the information presented in Competent Authority Reports for boric acid and disodium tetraborate .

## Risk assessment for human health

The biocidal product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat has been tested from toxicological point of view. However, information about toxicokinetics, critical endpoints and assessment factors presented in this section are taken from the final CARs on boric acid and disodium tetraborate to which the letter of access form the EBA A.I.S.B.L. has been submitted.

### Hazard potential

#### Toxicology of the active substance

Critical endpoints and assessment factors

Overall NOAEL

The toxicological data base reveals that the major targets for toxicity of borates are the testes and the blood. In the repeated dose studies with mouse, rat and dog, consistently effects on the testes and on blood parameters were found. In a 90 days study in the mouse the animals appeared to be more sensitive to the effects on the haematopoietic system than on the testes. In the rat effects on both the testes and on the blood were observed at dose levels of 334 mg boric acid/kg b.w./day. The NOAEL in this study was 100 mg/kg b.w./day (17.5 mg B/kg b.w./day). Similar results were obtained from studies with disodium tetraborate decahydrate at equimolar doses of boron. Based on the NOAEL for embryotoxic/teratogenic effects of boric acid of 55 mg/kg b.w./day (9.6 mg B/kg b.w./day) the overall NOAEL is 9.6 mg B/kg b.w./day.

Total assessment factor

The available information on kinetics and dynamics does not allow refinement of the standard assessment factors (10 for interspecies variation and 10 for intraspecies variation). There are indications that the sensitivity for the effects on the testes does not differ markedly between subchronic and chronic exposure. Therefore the application of an additional assessment factor for extrapolation from subchronic to chronic exposure is not required.

AOEL (acceptable operator exposure level)

Using the standard assessment factor of 100 (10 for interspecies- and 10 for intraspecies variation) an oral AOEL of 0.096 mg B/kg b.w./day can be derived based on the NOAEL for embryotoxic/teratogenic effects of boric acid of 9.6 mg B/kg b.w./day. Based on the NOAEL of 17.5 mg B/kg b.w./day in a 2-year study in the rat and an assessment factor of 300 due to serious effects and based on the NOAEL of 21.8 mg B/kg b.w./day in a teratogenicity study in the rabbit and an assessment factor of 300 due to serious effects AOEL values can be derived of 0.06 and 0.07 mg B/kg b.w./day, respectively. For the risk assessment, a rounded (systemic) AOEL value of 0.1 mg B/kg b.w./day was used, even though values of 0.06 and 0.07 mg B/kg b.w./day could be derived from the critical effects.

MOE (margin of exposure)

For the risk assessment of borates the systemic NOAEL of 9.6 mg/kg b.w./day will be used. A MOE of 100 would be considered acceptable, on the basis of the standard assessment factors of 100 (10 × 10) for interspecies and intraspecies variability.

#### Toxicology of the substance(s) of concern

The biocidal product contains one substance of concern – quaternary ammonium compounds, benzyl-C12-14-alkyldimethyl, chlorides (CAS 85409-22-9), trade name Barquat MS 100, classified and labeled under CLP regulation 1272/2008. The Barquat MS 100 concentration in the product is very low (0.66%) and does not affect on overall classification.

#### Toxicology of the biocidal product

Toxicokinetics

Absorption of borates via the oral route is nearly 100%. For the respiratory route also 100% absorption is assumed. Dermal absorption through intact skin is very low. For risk assessment of borates a dermal absorption of 0.5% is used. In the blood boric acid is the main species present. Boric acid is not further metabolised. Boric acid is distributed rapidly and evenly through the body, with concentrations in bone 2-3 higher than in other tissues. Boron is excreted relatively rapidly with elimination half-lives of 1h in the mouse, 3h in the rat and 21h in humans, and has low potential for accumulation. Boric acid is mainly excreted in the urine.

Acute toxicity

The biocidal product is of low acute toxicity: LD50 oral rat > 2000 mg/kg; LD50 dermal rat >2000 mg/kg.

Irritation and Corrosivity

The biocidal product is not a skin irritant or an eye irritant.

Sensitization

The biocidal product is non sensitizer, on the basis of a guinea pig maximization test.

The toxicology of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat was examined according to standard requirements.

The toxicological properties of the active substances are summarised in the respective CA reports:

- Boric acid - RMS NL 2009,

- Disodium tetraborate – RMS NL, 2008

No new data were provided on Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. The criteria for the classification of mixtures according to the Regulation 1272/2008 (CLP) were followed and accordingly, Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat  needs to be classified for Repr. 1B.

Skin corrosion and irritation

| Conclusion used in Risk Assessment – Skin corrosion and irritation |
| --- |
| Value/conclusion | Not harmful |
| Justification for the value/conclusion | The substance of concern (0.13%) is classified for skin irritant 2. Using the guidance for classifying mixtures under Regulation 1272/2008 (CLP), the biocidal product does not need to be classified for skin irritation 2 as the concentration is < 1%. |
| Classification of the product according to CLP and DSD | According to CLP no classification for skin irritation is necessary. |

| Data waiving |
| --- |
| Information requirement | Study scientifically unjustified |
| Justification | The toxicity of the active substances is known. Thus, toxicological properties and classification of the Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat can be deduced from the respective properties of the a.s. using the guidance for classifying mixtures under Regulation 1272/2008 (CLP). |

Eye irritation

| Conclusion used in Risk Assessment – Eye irritation |
| --- |
| Value/conclusion | Not harmful |
| Justification for the value/conclusion | The substance of concern (0.13) is classified for eye damage 1. Using the guidance for classifying mixtures under Regulation 1272/2008 (CLP), the biocidal product does not need to be classified for eye irritation as the concentration of substance of concern is < 1%. |
| Classification of the product according to CLP and DSD | According to CLP, no classification for eye irritation is necessary. |

| Data waiving |
| --- |
| Information requirement | Study scientifically unjustified |
| Justification | The toxicity of the active substances is known. Thus, toxicological properties and classification of the Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat can be deduced from the respective properties of the a.s. using the guidance for classifying mixtures under Regulation 1272/2008 (CLP). |

Respiratory tract irritation

| Conclusion used in the Risk Assessment – Respiratory tract irritation |
| --- |
| Value/conclusion | Not irritating to the respiratory tract. |
| Justification for the conclusion | A study for respiratory tract irritation with Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat has not been conducted. None of the active substances is classified as respiratory tract irritant. |
| Classification of the product according to CLP and DSD | According to CLP no classification for respiratory irritation is necessary. |

| Data waiving |
| --- |
| Information requirement | Study scientifically unjustified |
| Justification | The toxicity of the active substances is known. Thus, toxicological properties and classification of the Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat can be deduced from the respective properties of the a.s. using the guidance for classifying mixtures under Regulation 1272/2008 (CLP). |

Skin sensitization

| Conclusion used in Risk Assessment – Skin sensitisation |
| --- |
| Value/conclusion | Not sensitizing |
| Justification for the value/conclusion | None of the active substances is classified as skin sensitizer. |
| Classification of the product according to CLP and DSD | Not sensitising according to Regulation 1272/2008 (CLP). |

| Data waiving |
| --- |
| Information requirement | Study scientifically unjustified |
| Justification | The toxicity of the active substances is known. Thus, toxicological properties and classification of the Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat can be deduced from the respective properties of the a.s. using the guidance for classifying mixtures under Regulation 1272/2008 (CLP). |

Respiratory sensitisation (ADS)

| Conclusion used in Risk Assessment – Respiratory sensitisation |
| --- |
| Value/conclusion | Not sensitising for the respiratory tract. |
| Justification for the value/conclusion | Respiratory sensitization studies with Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat have not been conducted. According to BPR guidance on human health risk assessment, it is plausible to suspect skin sensitizers for also being sensitising to the respiratory tract. None of the active substances is classified as skin sensitizer. |
| Classification of the product according to CLP and DSD | Not sensitising to the respiratory tract according to Regulation 1272/2008 (CLP). |

| Data waiving |
| --- |
| Information requirement | Study scientifically unjustified |
| Justification | The toxicity of the active substances is known. Thus, toxicological properties and classification of the Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat can be deduced from the respective properties of the a.s. using the guidance for classifying mixtures under Regulation 1272/2008 (CLP). |

Reproductive toxicity

| Conclusion used in Risk Assessment – reproductive toxicity |
| --- |
| Value/conclusion | Toxic |
| Justification for the value/conclusion | Reproductive toxicity studies with Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat have not been conducted. The active substances disodium tetraborate (5%) and boric acid (15%) are classified as reproduction toxicant and specific concentration limits have been exceeded for both a. s. in accordance with the 1th ATP (corrected) to CLP (Commission Regulation (EU) 2018/669 of 16 April 2018). The concentration of disodium tetraborate is above the concentration limit of 4.5% and the concentration of boric acid is also above the concentration limit of 5.5%. |
| Classification of the product according to CLP and DSD | According to CLP, classification for reproductive toxicity is necessary, Repr. 1B, H360FD. |

| Data waiving |
| --- |
| Information requirement | Study scientifically unjustified |
| Justification | The toxicity of the active substances is known. Thus, toxicological properties and classification of the Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat can be deduced from the respective properties of the a.s. using the guidance for classifying mixtures under Regulation 1272/2008 (CLP). |

Acute toxicity

Acute toxicity by oral route

| Value used in the Risk Assessment – Acute oral toxicity |
| --- |
| Value | Not harmful |
| Justification for the selected value | The substance of concern is classified for acute oral toxicity 3. Using the guidance for classifying mixtures under Regulation 1272/2008 (CLP), the biocidal product does not need to be classified for acute oral toxicity as ATEmix is > 2000 mg/kg. |
| Classification of the product according to CLP and DSD | According to CLP, classification for acute oral toxicity is unnecessary. |

| Data waiving |
| --- |
| Information requirement | Study scientifically unjustified |
| Justification | The toxicity of the active substances is known. Thus, toxicological properties and classification of the Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat can be deduced from the respective properties of the a.s. using the guidance for classifying mixtures under Regulation 1272/2008 (CLP). |

Acute toxicity by inhalation

| Value used in the Risk Assessment – Acute inhalation toxicity |
| --- |
| Value | Not harmful |
| Justification for the selected value | Acute toxicity studies with Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat have not been conducted. None of the active substances is classified as respiratory sensitizer or toxicant by inhalation. |
| Classification of the product according to CLP and DSD | According to CLP, no classification for acute inhalation toxicity is necessary. |

| Data waiving |
| --- |
| Information requirement | Study scientifically unjustified |
| Justification | The toxicity of the active substances is known. Thus, toxicological properties and classification of the Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat can be deduced from the respective properties of the a.s. using the guidance for classifying mixtures under Regulation 1272/2008 (CLP). |

Acute toxicity by dermal route

| Value used in the Risk Assessment – Acute dermal toxicity |
| --- |
| Value | Not harmful |
| Justification for the selected value | The substance of concern is classified for acute dermal toxicity 3. Using the guidance for classifying mixtures under Regulation 1272/2008 (CLP), the biocidal product does not need to be classified for acute dermal toxicity as ATEmix is > 2000 mg/kg. |
| Classification of the product according to CLP and DSD | No classification according to Regulation (EC) No 1272/2008. |

| Data waiving |
| --- |
| Information requirement | Study scientifically unjustified |
| Justification | The toxicity of the active substances is known. Thus, toxicological properties and classification of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat can be deduced from the respective properties of the a.s. using the guidance for classifying mixtures under Regulation 1272/2008 (CLP). |

### Exposure

The exposure to borates is calculated by using the selected models and default values for wood preservatives from the User Guidance TNsGas a guideline. In the calculations the process information given by the notifier is used as a base for the calculation.

Main paths of human exposure:

| Route of exposure | Industrial use | Professional user | Via the environment |
| --- | --- | --- | --- |
| inhalation | Yes | Yes | No |
| dermal | Yes | Yes | No |
| oral | No | No | No |

The crucial exposure is connected with mixing process, because the product ready to use is not classified and no adverse health effects are expected.

Direct contact with concentrated formulations of biocidal product should be avoided at each step. Where possible, use a container which avoids splashing, and/or small hand transfer pumps and/or pouring cradles. Concentrate should be diluted to 20% water solution ready to use where controlled conditions can be maintained and not where the public have access. Containers for diluted products must be suitably labelled. To minimize the exposure by inhalation and through the skin to concentrate appropriate protective clothing (gloves, coveralls, and foot protection) and respiratory protection should be provided and worn by worker when at each step of using the product. The secondary (indirect) exposure occurs after the actual use or application of the biocidal product. Secondary exposure to the non-users results from contact with treated timber/wood; e.g. adults using preserved timber in construction.

The treated wood is not placed on the market until it is dry. Use of biocidal product on wood, which is likely to come into prolonged direct contact with foodstuffs or feedstuffs is not expected.

Indirect exposure via the environment is considered not relevant based upon the rapid environmental degradation of biocidal product ingredients.

#### Exposure of industrial and professional users

Assumptions used in the estimations of exposure:

- the total content of active substances in Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is 20% w/w and in product ready to use is 4% w/w,

- the total content of active substances in Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat expressed as B equivalents is 15% boric acid × 0.175 + 5% disodium tetraborate × 0.215 = 0.037 B equivalents

- the total content of active substances in product ready to use expressed as B equivalents is 3% boric acid × 0.175 + 1% disodium tetraborate × 0.215 = 0.0074 B equivalents

- default factor 0.1 for the use of PPE

- rate and extent of dermal absorption: 0.5%

- rate and extent of inhalation absorption: 100%

- body weight 60 kg

##### Vacuum pressure

Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is diluted to 20% water solution as a product ready to use. Exposure is related to the following steps:

Step 1a. Mixing and loading(the dose effective to protect wood against insects and fungi)

The exposure is calculated by using models and default values for wood preservatives from the User Guidance TNsG as a guideline. Exposure is assessed based on the model ‘Mixing and Loading: Model 5’ (95th percentile; TNsG):

- potential dermal exposure for powder  – 14.3 mg a.s./kg a.s.

- potential inhalation exposure for powder – 0.55 mg a.s./kg a.s.

- application rate – 5 kg of product /m3 wood = 0.185 kg B/m3 wood (recommended by the Applicant)

- treated wood – 30 m3 wood/day ESD,

- in ‘Mixing and Loading: Model 5’ no information about exposure with PPE is given, therefore the default factor for exposure with and without PPE of 0.1, which is common practice in the UE, is used for both the dermal and the inhalation exposure with PPE.

Chronic systemic exposure during mixing and loading:

- without PPE

dermal exposure: 79.37mg B/day × 0.005 = 0.40 mg B/day = 0.0067 mg B/kg b.w./day

inhalation exposure: 3.05 mg B/day × 1 = 3.05 mg B/day = 0.0508 mg B/kg b.w./day

- with PPE

dermal exposure: 0.00067 mg B/kg b.w./day

inhalation exposure: 0.00508 mg B/kg b.w./day.

Step 1b. Mixing and loading (the highest dose proposed by the applicant for this type of application)

The exposure is calculated by using models and default values for wood preservatives from the User Guidance TNsG as a guideline. Exposure is assessed based on the model ‘Mixing and Loading: Model 5’ (95th percentile; TNsG):

- potential dermal exposure for powder  – 14.3 mg a.s./kg a.s.,

- potential inhalation exposure for powder – 0.55 mg a.s./kg a.s.,

- application rate – 40 kg of product /m3 wood = 1.48  kg B/m3 wood (recommended by the Applicant),

- treated wood – 30 m3 wood/day ESD,

- in ‘Mixing and Loading: Model 5’ no information about exposure with PPE is given, therefore the default factor for exposure with and without PPE of 0.1, which is common practice in the UE, is used for both the dermal and the inhalation exposure with PPE.

Chronic systemic exposure during mixing and loading:

- without PPE

dermal exposure: 634.92 mg B/day × 0.005 = 3.17 mg B/day = 0.053 mg B/kg b.w./day

inhalation exposure: 24.42 mg B/day × 1 = 24.42 mg B/day = 0.407 mg B/kg b.w./day

- with PPE

dermal exposure: 0.0053 mg B/kg b.w./day

inhalation exposure: 0.0407 mg B/kg b.w./day

Step 2. Application and post-application

The exposure is calculated by using models and default values for wood preservatives from the User Guidance TNsG as a guideline. Exposure is assessed based on the model ‘Handling: Model 1’ (water based; 75th percentile; TNsG).

- potential dermal exposure – 8570 mg of product ready to use/cycle,

- for vacuum pressure process: daily use 3 cycles/day and 3 hours/cycle ,

- probability of exposure by inhalation – 1.9 mg of product ready to use/m3,

- inhalation rate – 0.021 m3/min,

- during the application and post-application phase gloves, coverall and respiratory protective equipment are used. In ‘Handling: Model 1’ the dermal exposure inside gloves and inside shoes is described, which is approximately 18% of the potential dermal exposure. The exposure inside gloves and inside shoes certainly isn’t the total dermal exposure with PPE. Therefore, the default factor of 0.1, which is common practice in the UE and stated in the TNsG.

Chronic systemic exposure:

- without PPE

dermal exposure: 190.25 mg B/day × 0.005 = 0.95 mg B/day = 0.016 mg B/kg b.w./day

inhalation exposure: 0.16 mg B/day × 1 = 0.16 mg B/day = 0.0026 mg B/kg b.w./day

- with PPE

dermal exposure: 0.0016 mg B/kg b.w./day

inhalation exposure: 0.00026 mg B/kg b.w./day

##### Dipping

Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is diluted to 20% water solution as a product ready to use. Exposure is related to the following steps:

Step 1. Mixing and loading (the dose effective to protect wood against insects and fungi)

The exposure is calculated by using models and default values for wood preservatives from the User Guidance TNsG as a guideline.

Exposure is assessed based on the model ‘Mixing and Loading: Model 5’ (95th percentile; TNsG):

- potential dermal exposure for powder  – 14.3 mg a.s./kg a.s.,

- potential inhalation exposure for powder – 0.55 mg a.s./kg a.s.,

- application rate – 5 kg of product /m3 wood = 0.185 kg B/m3 wood (recommended by the Applicant),

- treated wood – 100 m3 wood/day    ESD,

- in ‘Mixing and Loading: Model 5’ no information about exposure with PPE is given, therefore the default factor for exposure with and without PPE of 0.1, which is common practice in the UE, is used for both the dermal and the inhalation exposure with PPE.

Chronic systemic exposure during mixing and loading:

- without PPE

dermal exposure: 264.55 mg B/day × 0.005 = 1.32 mg B/day = 0.022 mg B/kg b.w./day

inhalation exposure: 10.18 mg B/day × 1 = 10.18 mg B/day = 0.17 mg B/kg b.w./day

- with PPE

dermal exposure: 0.0022 mg B/kg b.w./day

inhalation exposure: 0.017 mg B/kg b.w./day

Step 2a. Application and post-application (manual dipping)

The exposure is calculated by using models and default values for wood preservatives from the User Guidance TNsG as a guideline. Exposure is assessed based on the model ‘Dipping: Model 1’ (75th percentile; TNsG).

- potential dermal exposure – 178 mg of product ready to use/min,

- for dipping process: up to 30 min immersion/batch,

- 5 cycles/day (according to Applicant),

- during the application and post-application phase gloves and a coverall are used and no respiratory protective equipment. In ‘Dipping: Model 1’ the exposure with PPE is not stated, only the exposure inside gloves and inside shoes, which is approximately 9.9% of the potential dermal exposure. The exposure inside gloves and inside shoes certainly isn’t the total dermal exposure with PPE. Therefore, the default factor of 0.1, which is common practice in the UE and stated in the TNsG,

- in ‘Dipping: Model 1’ no range of non-zero values is given for the exposure by inhalation; all 5 data for inhalation were zero values.

Chronic systemic exposure:

- without PPE

197.58 mg B/day × 0.005 = 0.99 mg B/day = 0.017 mg B/kg b.w./day

- with PPE

0.0017 mg B/kg b.w./day

Step 2b. Application and post-application (automated dipping)

The exposure is calculated by using models and default values for wood preservatives from the User Guidance TNsG as a guideline. Exposure is assessed based on the model ‘Handling: Model 1’ (water based; 75th percentile; TNsG).

- potential dermal exposure – 8570 mg of product ready to use/cycle,

- for automated dipping process: daily use 4 cycles/day  and 1 hour/cycle,

- during the application and pos-application phase gloves and a coverall are used and no respiratory protective equipment. In ‘Handling: Model 1’ the dermal exposure inside gloves and inside shoes is described, which is approximately 18% of the potential dermal exposure. The exposure inside gloves and inside shoes certainly isn’t the total dermal exposure with PPE. Therefore, the default factor of 0.1, which is common practice in the UE and stated in the TNsG.

Chronic systemic exposure:

- without PPE

dermal exposure: 253.67 mg B/day × 0.005 = 1.27 mg B/day = 0.021 mg B/kg b.w./day

- with PPE

dermal exposure: 0.0021 mg B/kg b.w./day

##### Painting/brushing:

Step 1a. Mixing and loading (the dose effective to protect wood against insects and fungi)

The exposure is calculated by using models and default values for wood preservatives from the User Guidance TNsG as a guideline. Exposure is assessed based on the model ‘Mixing and Loading: Model 5’ (95th percentile; TNsG). However, due to the fact that certain value (for which the applicant did not submitted the access) was used in the calculation by RMS, full calculations were placed in Annex 8 as a confidential.

Chronic systemic exposure during mixing and loading:

- without PPE

dermal exposure: 0.53 mg B/day × 0.005 = 0.0027 mg B/day = 0.000045 mg B/kg b.w./day

inhalation exposure: 0.02 mg B/day × 1 = 0.02 mg B/day = 0.00033 mg B/kg b.w./day

- with PPE

dermal exposure: 0.0000045 mg B/kg b.w./day

inhalation exposure: 0.000033 mg B/kg b.w./day

Step 1b. Mixing and loading (the highest dose proposed by the applicant for this type of application)

The exposure is calculated by using models and default values for wood preservatives from the User Guidance TNsG as a guideline. Exposure is assessed based on the model ‘Mixing and Loading: Model 5’ (95th percentile; TNsG). However, due to the fact that certain value (for which the applicant did not submitted the access) was used in the calculation by RMS, full calculations were placed in Annex 9 as a confidential.

Chronic systemic exposure during mixing and loading:

- without PPE

dermal exposure: 1.058 mg B/day × 0.005 = 0.0053 mg B/day = 0.000088 mg B/kg b.w./day

inhalation exposure: 0.0407 mg B/day × 1 = 0.0407 mg B/day = 0.00068 mg B/kg b.w./day

- with PPE

dermal exposure: 0.0000088  mg B/kg b.w./day

inhalation exposure: 0.000068 mg B/kg b.w./day

Step 2. Application

The exposure is calculated by using models and default values for wood preservatives from the User Guidance TNsG as a guideline. There are no exposure models for professional painters, therefore, the exposure is assessed based on the model ‘Consumer Product Painting: Model 3’ (75th percentile; TNsG).

- potential dermal exposure is 16.9 mg product/min,

- use 4 hours/day (see: User Guidance TNsG), the use of preservative by professionals is less than half the time spent at the job),

- potential inhalation exposure – 4.15 mg of product ready to use/m3,

- inhalation rate – 0.021 m3/min,

- during the application and post-application phase gloves, coverall and respiratory protective equipment are used. In ‘Consumer Product Painting: Model 3’ the exposure with PPE is not stated, only the exposure inside gloves and inside shoes, which is approximately 5.8 % of the potential dermal exposure. The exposure inside gloves and inside shoes certainly isn’t the total dermal exposure with PPE. Therefore, the default factor of 0.1, which is common practice in the UE and stated in the TNsG, is used as reduction factor.

Chronic systemic exposure:

- without PPE

dermal exposure: 30.1 mg B/day × 0.005 = 0.15 mg B/day = 0.0025 mg B/kg b.w. /day

inhalation exposure: 0.15 mg B/day ×1 =0.15 mg B/day = 0.0025 mg B/kg b.w./day

- with PPE

dermal exposure: 0.00025 mg B/kg b.w./day

inhalation exposure: 0.00025 mg B/kg b.w./day

#### Non-professional exposure

Not relevant. The biocidal product is intended only for professional and industrial use.

#### Indirect exposure as a result of use of the active substance in biocidal product

Indirect exposure to borates as a result of use can occur during cutting and sanding and during handling treated timber. Exposure can take place due to inhalation of sawdust and due to contact with the treated wood.

Industrial treatment of timber occurs in large industrial installations. The indirect exposure does not occur at these industrial sites but elsewhere. In fact, this is exposure to a treated product. Here the exposure during cutting and sanding industrial treated timber will be described for professionals and non-professionals.

In the User Guidance TNsG the example Wood Preservatives’ provides ‘reference scenarios’ for calculating exposure during cutting and sanding by professionals and non-professionals. These ‘reference scenarios’ are used as starting point for the exposure assessment.

Besides when handling timber, exposure could as well occur during the use of timber treated with wood preservatives. Treated timber could be used for playground structures outdoors but under cover where high environmental humidity can lead to occasional wetting. Children playing at these constructions could be exposed to borates by contacting the wood. In the User Guidance TNsG a ‘reference scenario’ for children playing on playground structures outdoors is described. This scenario will be starting point of the exposure assessment.

The ’indirect exposure as a result of use’ is mainly based on assumptions and not on measurements nor on default values derived from measurements. Therefore the result of the exposure assessment must be seen as an indication of the order of magnitude.

##### Exposure during cutting and sanding by professionals

Scenario: Adult (-professional) sanding (powered sander) wooden posts (4 cm × 4 cm × 2.5 m) for one hour. The posts have been treated with wood preservative solution by the vacuum process (200 kg of product ready to use/m3 wood). Sanding of treated wood occurs every work day.

Inhalation exposure

Active substance in the posts = 200 kg of product ready to use/m3 wood = 1.48 kg B/m3 wood = 1.48 mg B/cm3 wood

Wood density: 0.5 g/cm3 (according to Assessment Report for boric acid)

In the posts: 1.48 mg B/cm3 wood/0.5 g/cm3 = 2.96 mg B/g wood = 0.00296 mg B/mg wood

Inhalation rate: 1.25 m3 air /hour

If the inhalation exposure were to be 5 mg/m3 (equal to the occupational exposure limit for wood dust) the inhalation exposure = 5 mg/m3 × 1.25 m3/hour × 1 hour/day = 6.25 mg wood dust/day.

Inhalation exposure:

6.25 [mg wood dust/day] × 0.00296 mg B/mg wood = 0.0185 mg B/day of exposure

Inhalation absorption factor 1

Internal chronic inhalation exposure: 0.0185 mg [B / day of exposure] × 1 [absorption factor] / 60 [kg b.w.] = 0.00031 mg B/(kg b.w. × day).

Dermal exposure

Active substance residue on surface = 1 mg/cm2 = 0.0074 mg B/cm2

Hand surface area = 420 cm2

Assume 20% of hand (84 cm2) contaminated at 100% of surface concentration

Dermal exposure = 0.0074 × 84 = 0.62 mg B/day of exposure

Dermal absorption factor: 0.005

Internal chronic dermal exposure = 0.62 [mg B/day of exposure] × 0.005 [absorption factor] / 60 [kg b.w.] = 0.000052 mg B/(kg b.w. × day).

##### Exposure during cutting and sanding by non-professionals

Scenario: Adult (non-professional) sanding (powered sander) wooden posts (4 cm × 4 cm × 2.5 m) for one hour. The posts have been treated with wood preservative solution by the vacuum process (200 kg of product ready to use/m3 wood). Sanding of treated wood by non-professional occurs once a year.

Inhalation exposure

Active substance in the posts = 200 kg of product ready to use/m3 wood = 1.48 kg B/m3 wood = 1.48 mg B/cm3 wood

Wood density: 0.5 g/cm3 (according to Assessment Report for boric acid)

In de posts: 1.48 mg B/cm3 wood/0.5 g/cm3 = 2.96 mg B/g wood = 0.00296 mg B/mg wood

Inhalation rate: 1.25 m3 air /hour

If the inhalation exposure were to be 5 mg/m3 (equal to the occupational exposure limit for wood dust) the inhalation exposure = 5 mg/m3 × 1.25 m3/hour × 1 hour/day = 6.25 mg wood dust/day.

Inhalation exposure:

6.25 [mg wood dust/day] × 0.00296 mg B/mg wood = 0.0185 mg B/day of exposure

Inhalation absorption factor 1

Internal inhalation exposure (acute): 0.0185 mg [B / day of exposure] × 1 [absorption factor] / 60 [kg b.w.] = 0.00031 mg B/(kg b.w. × day).

Dermal exposure

Active substance residue on surface = 1 mg/cm2 = 0.0074 mg B/cm2

Hand surface area = 420 cm2

Assume 20% of hand (84 cm2) contaminated at 100% of surface concentration

Dermal exposure = 0.0074 × 84 = 0.62 mg B/day of exposure

Dermal absorption factor: 0.005

Internal dermal exposure (acute) = 0.62 [mg B/day of exposure] × 0.005 [absorption factor] / 60 [kg b.w.] = 0.000052 mg B/(kg b.w. × day).

##### Exposure of a child playing on playground structure outdoors

Scenario: Child playing on playground structure outdoors but under cover where high environmental humidity can lead to occasional wetting. The structures are made of wood, which has been treated with wood preservative and there is prolonged and repeated contact of wood with hands, which causes dermal exposure. Oral exposure may occur via hand-to-mouth transfer. It is assumed that 10% of the dermal exposure to borates is ingested orally due to hand-to-mouth transfer.

Child, 2-5 years of age, 16.7 kg.

Exposure hands

Surface loading of boron in treated wood: 0.01 mg/cm2 wood × 0.0074 B equivalents = 0.000074 mg B/cm2

Hand surface area = 200 cm2

Assume 20% of hand (40 cm2) contaminated at 100% of surface concentration

Total exposure on the hands = 0.000074 × 40 = 0.003 mg B/day

It is assumed that 10% of the total exposure that ends up on the skin of a child is taken in orally due to hand-mouth contact.

Dermal exposure 0.9 × 0.003 = 0.0027 mg B/day

Dermal absorption factor: 0.005

Internal chronic dermal exposure = 0.0027 [mg B/day of exposure] × 0.005 / 16.7 [kg b.w.] = 0.00000081 mg B/(kg b.w. × day).

Oral exposure due to hand-mouth contact: 0.1 × 0.003 = 0.0003 mg B/day

Oral absorption factor: 1

Internal chronic oral exposure = 0.0003 [mg B/day of exposure] / 16.7 [kg b.w.] = 0.000018 mg B/(kg b.w. × day)

Exposure of a toddler or a child playing on playground structure outdoors

Scenario: Toddler or child playing on playground structure outdoors but under cover where high environmental humidity can lead to occasional wetting. The structures are made of wood, which has been treated with wood preservative and there is prolonged and repeated contact of wood with hands, which causes dermal exposure. Oral exposure may occur via hand-to-mouth transfer. It is assumed that 10% of the dermal exposure to borates is ingested orally due to hand-to-mouth transfer.

Toddler, 2 years of age, 10 kg.

Exposure hands

Surface loading of boron in treated wood: 0.01 mg/cm2 wood × 0.0074 B equivalents = 0.000074 mg B/cm2

Hand surface area = 115.2 cm2

Assume 20% of hand (23.04 cm2) contaminated at 100% of surface concentration

Total exposure on the hands = 0.000074 × 23.04 = 0.0017 mg B/day

It is assumed that 10% of the total exposure that ends up on the skin of a child is taken in orally due to hand-mouth contact.

Dermal exposure 0.9 × 0.0017 = 0.0015 mg B/day

Dermal absorption factor: 0.005

Internal chronic dermal exposure = 0.0015 [mg B/day of exposure] × 0.005 / 10 [kg b.w.] = 0.00000077 mg B/kg b.w./day

Oral exposure due to hand-mouth contact: 0.1 × 0.0017 = 0.00017 mg B/day

Oral absorption factor: 1

Internal chronic oral exposure = 0.00017 [mg B/day of exposure] / 10 [kg b.w.] = 0.000017 mg B/kg b.w./day

### Risk Characterisation

The risk characterization was performed in accordance with the recommendations of the technical guidelines TNsG (Annex I Inclusion Revision of Charter 4.1: Quantitative Human Health Risk Characterisation), based on the determined values of MOE and AEL.

#### Risk for industrial and professional users

Table 2.6 Risk assessment of biocidal product

| Exposure | Estimated exposure [mg B/kg b.w./day] | AOEL systemic [mg B/kg b.w./day] | Risk index |
| --- | --- | --- | --- |
|  | without PPE | with PPE |  | without PPE | with PPE |
| Vacuum pressure impregnation (the dose effective to protect wood against insects and fungi) | 0.0761 | 0.00761 | 0.1 | 0.761 | 0.0761 |
| Vacuum pressure impregnation (the highest dose proposed by the applicant for this type of application) | 0.4786 | 0.04786 | 0.1 | 4.786 | 0.4786 |
| Manual dipping | 0.209 | 0.0209 | 0.1 | 2.09 | 0.209 |
| Automated dipping | 0.213 | 0.0213 | 0.1 | 2.13 | 0.213 |
| Painting/brushing (the dose effective to protect wood against insects and fungi) | 0.005375 | 0.0005375 | 0.1 | 0.05375 | 0.005375 |
| Painting/brushing (the highest dose proposed by the applicant for this type of application) | 0.005768 | 0.0005768 | 0.1 | 0.05768 | 0.005768 |

| Table 2.7 Risk assessment of biocidal product |
| --- |
| Exposure | Estimated exposure [mg B/kg b.w./day] | NAOEL systemic [mg B/kg b.w./day] | MOE |
|  | without PPE | with PPE |  | without PPE | with PPE |
| Vacuum pressure impregnation (the dose effective to protect wood against insects and fungi) | 0.0761 | 0.00761 | 9.6 | 126 | 1261 |
| Vacuum pressure impregnation (the highest dose proposed by the applicant for this type of application) | 0.4786 | 0.04786 | 9.6 | 20 | 201 |
| Manual dipping | 0.209 | 0.0209 | 9.6 | 46 | 4595 |
| Automated dipping | 0.213 | 0.0213 | 9.6 | 45 | 451 |
| Painting/brushing (the dose effective to protect wood against insects and fungi) | 0.005375 | 0.0005375 | 9.6 | 1786 | 17860 |
| Painting/brushing (the highest dose proposed by the applicant for this type of application) | 0.005768 | 0.0005768 | 9.6 | 1664 | 16644 |

It can be concluded that adverse health effects for the unprotected industrial and professional users due to combined dermal and respiratory exposure of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, as a result of the processes as described in the Table 2.6 and Table 2.7 cannot be excluded in the case of vacuum pressure impregnation (the highest dose proposed by the applicant for this type of application), manual and automated dipping processes. Protective clothing (gloves, coveralls, and foot protection) and respiratory protection are necessary to reduce the exposure to get risk indices < 1 and the MOEs > 100.

In connection with above, PPE are required in the case of vacuum pressure impregnation (the highest dose proposed by the applicant for this type of application), manual and automated dipping processes, however in case of other processes using the PPE is also recommended.

#### Indirect exposure as a result of use of the active substance in biocidal product

Table 2.8 Risk assessment of biocidal product without PPE

| Exposure | Estimated exposure [mg B/kg b.w./day] | AOEL systemic [mg B/kg b.w./day] | Risk index |
| --- | --- | --- | --- |
| Exposure during cutting and sanding by professionals | 0.000362 | 0.1 | 0.00362 |
| Exposure during cutting and sanding by non-professionals | 0.000362 | 0.1 | 0.00362 |
| Exposure of a child playing on playground structure outdoors | 0.0000188 | 0.1 | 0.000188 |
| Table 2.9 Risk assessment of biocidal product without PPE |
| Exposure | Estimated exposure [mg B/kg b.w./day] | AOEL systemic [mg B/kg b.w./day] | Risk index |
| Exposure during cutting and sanding by professionals | 0.000362 | 9.6 | 26519 |
| Exposure during cutting and sanding by non-professionals | 0.000362 | 9.6 | 26519 |
| Exposure of a child playing on playground structure outdoors | 0.0000188 | 9.6 | 510367 |

Table 2.8 Risk assessment of biocidal product without PPE

| Exposure | Estimated exposure [mg B/kg b.w./day] | AOEL systemic [mg B/kg b.w./day] | Risk index |
| --- | --- | --- | --- |
| Exposure during cutting and sanding by professionals | 0.000362 | 0.1 | 0.00362 |
| Exposure during cutting and sanding by non-professionals | 0.000362 | 0.1 | 0.00362 |
| Exposure of a child playing on playground structure outdoors | 0.0000178 | 0.1 | 0.000178 |
| Table 2.9 Risk assessment of biocidal product without PPE |
| Exposure | Estimated exposure [mg B/kg b.w./day] | AOEL systemic [mg B/kg b.w./day] | MOE |
| Exposure during cutting and sanding by professionals | 0.000362 | 9.6 | 26519 |
| Exposure during cutting and sanding by non-professionals | 0.000362 | 9.6 | 26519 |
| Exposure of a child playing on playground structure outdoors | 0.0000178 | 9.6 | 539 325 |

No adverse health effects for the non-professional user and the professional user due to indirect exposure are expected. For child playing on a playground structure outdoors (but under cover where high environmental humidity can lead to occasional wetting) a health risk as a consequence of exposure to borates can be excluded.

## Risk assessment for the environment

Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is use as a wood preservative against wood destroying basidiomycetes and wood boring beetle.

Biocidal product is intended to use in use class 1 (UC1 – timber under cover and fully protected from the weather, not exposed to wetting) and in use class 2 (UC2 – timber under cover and fully protected from the weather but where high environmental humidity can lead to occasional but not persistent wetting).

### Fate and distribution in the environment

The biocidal product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat contains two active substances: 15% w/w of boric acid and 5% w/w disodium tetraborate and is dissolved with water to final concentration of 20% which contains 3% w/w of boric acid and 1% w/w of disodium tetraborate

Biocidal product contain also one substance of concern – quaternary ammonium compounds, benzyl-C12-14-alkyldimethyl, chlorides (CAS 85409-22-9), trade name Barquat MS 100, classified and labelled under CLP regulation 1272/2008. The Barquat MS 100 concentration in the product is very low (0.66%) and does not affect on overall classification of product. Therefore only active substances are considered as of concern for environment and the risk characterisation can be performed only for these substances. Data necessary to assess risk for these substances were derived from the Competent Authority Report for boric acid and disodium tetraborate.

The characteristics of active substances including lists of endpoints are available in Competent Authority Reports for boric acid and disodium tetraborate. Applicant confirmed access to those data by the Letter of Access for boric acid and disodium tetraborate.

### Emission to environmental compartments

The product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat  is intended to used in UC1 and UC2. No emission scenarios are available for these Use Classes, since the potential risk from treated wood to the outer environment is considered negligible. Therefore, there is no necessity to assess the environmental risk.

In the case of application and storage of treated wood prior to shipment, the Annex I inclusion directives for both boric acid and disodium tetraborate include the following specific provision:

“In particular, labels and/or safety-data sheets of products authorised for industrial use shall indicate that freshly treated timber must be stored after treatment under shelter and/or on impermeable hard standing to prevent direct losses to soil or water and that any losses must be collected for reuse or disposal.”

Since for UC1 and UC2 the potential emission to the environment from treated wood in service is considered negligible and losses from storage of treated wood must be prevented, treatment process is the only phase considered in estimation of emission.

Emission, fate and behaviour in the environment were considered jointly for boric acid and disodium tetraborate because disodium tetraborate are converted into boric acid/borate upon dissolution in water. The same way as in Competent Authority Reports for active substances it is assumed that boric acid will be the predominant species in environmental compartments. Predicted Environmental Concentrations of active substances in environmental compartments (PEC’s) were converted to boron concentration (for further explanation see Document IIB). These values were compared to Predicted No Effect Concentrations (PNEC’s) derived from Competent Authority Reports for boric acid and disodium tetraborate. PNEC’s values for both active substances were also expressed as concentration of boron.

It has to be noted that boron is present in natural environments. Therefore the PEC’s and PNEC’s mentioned in this document are PECadd’s and PNECadd’s, added concentrations on top of the background concentration, due to emission of boric acid to the environment.

.

In penetrating methods retention 2.5 kg of concentrate/m3 prevents the attack of rotting destroying fungi. The application rate 5kg/m3 (25 kg/m3 20% water solution) is effective for prevention of softwood against the fungi and insects together. Therefore application rate 5kg/m3 was used to calculate the emission.

Application rates for product containing boron compounds are expressed as boron equivalents. Application rate 185 g of boron per m3 of wood was used to calculate the emission.

According to declaration of Applicant biocidal product Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is a fire retardant. This is not evaluated by Polish Competent Authority because it is not biocidal activity. However for sake of completeness the highest application rate declared by Applicant (40 kg of product per m3 of wood) was considered in assessment. Application rate 1480 g of boron per m3 of wood was also used to calculate the emission. Moreover according to Applicant declaration only vacuum treatment is used to protect wood against fire. Therefore additional application rate is considered only in emission estimation during vacuum treatment.

There are no available scenarios for industrial painting/brushing. According to calculation performed by Polish Competent Authority emission during professional application is not higher than during automated processes. Exposure estimation for vacuum and dipping treatment covers emission for painting/brushing.

### Environmental risk assessment

#### Aquatic compartment

##### Surface water and sediment

According to the ESD industrial application of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat leads to exposure of surface water (for further explanation see Document IIB). Therefore risk must be estimated for this compartment.

A PNECadd, water of 180 µg B/L was derived from Competent Authority Reports for boric acid and disodium tetraborate. This value is compared with values of PECadd,water to estimate risk for surface waters.

Table 2.10 PECadd,water/PNECadd,water ratio for surface water and sediment

|  | PECadd,water [µg B/L] | PNECadd,water [µg B/L] | PEC/PNEC |
| --- | --- | --- | --- |
| Vacuum pressure | 8.3 | 180 | 0.046 |
| Vacuum pressure (fire retardant) | 66.4 | 180 | 0.369 |
| Automated dipping | 27.7 | 180 | 0.154 |

PECadd,water/PNECadd,water ratios for surface water associated with industrial application of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat are < 1 for all scenarios and application rates. Therefore, no aquatic risks are expected.

No PECadd,sediment/PNECadd,sediment values have been determined because the Polish Competent Authority has concluded that boron does not pose any significant threat to the sediment compartment. Boron has a low adsorption potential. Therefore this atom remains predominantly in the water phase and does not adsorb to sediment. Risk assessment for the sediment compartment is not needed, risk assessment for the aquatic compartment should sufficiently cover any sediment dwelling organisms as the route of exposure will be predominantly aquatic. Therefore, taking into consideration risk assessment for surface water, the Polish Competent Authority has concluded that the proposed use patterns would not result in an unacceptable risk to the sediment compartment.

##### Sewage treatment plant

A PNECadd,STP  of 1.8 mg B/L was derived from Competent Authority Reports for boric acid and disodium tetraborate. This value is compared with values of PECadd,STP to estimate risk for STP.

Table 2.11 PECadd,STP/PNECadd,STP ratio for sewage treatment plant

|  | PECadd,STP [µg B/L] | PNECadd,STP [mg B/L] | PEC/PNEC |
| --- | --- | --- | --- |
| Vacuum pressure | 83 | 1.8 | 0.046 |
| Vacuum pressure (fire retardant) | 664 | 1.8 | 0.369 |
| Automated dipping | 277 | 1.8 | 0.154 |

PECadd,STP/PNECadd,STP ratios for sewage treatment plant associated with industrial application of Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat are < 1 for all scenarios and application rates. Therefore, no risk for STP is expected.

#### Atmosphere

Due to the low volatility of the inorganic borates, emission to air is very low. Therefore estimation of risk for atmosphere is considered to be not necessary.

#### Terrestrial compartment

Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat is intended to be applied by industrial application processes vacuum, dipping and painting/brushing. According to ESD proposed application method and use of the biocidal product and taking into consideration fate and behavior of boric acid there is no potential exposure of terrestrial compartment and risk for soil.

#### Groundwater

According to Annex I, part B of the Council Directive 98/83/EC of 3 November 1998 on the quality of water intended for human consumption, there is a limit value for boron (as a representative for boric acid and tetraborates) is 1 mg B /l.

According to proposed use the biocidal product, Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat, there is no potential exposure, therefore consideration of risk for groundwater is not necessary.

### Non compartment specific effects relevant to the food chain  (secondary poisoning)

Boron is an essential micronutrient for all plants and is applied as an agricultural fertiliser. Borates are therefore part of an everyday diet of fresh fruit and vegetables. While boron may accumulate in plants and some animals relative to their immediate environment, there is evidence from field studies that boron is not bioconcentrated or bioaccumulated along the food chain (for further explanation please see Competent Authority Reports for boric acid and disodium tetraborate).

### Comparative assessment

PBT assessment has to be done according to the TGD especially for substances which reveal following features: both persistent for long periods and bioaccumulative in biota as well as can give toxic effects after a long-term exposure.

Substances which fulfil the PBT or vPvB criteria will not be included in Annex I unless release to the environment can be effectively prevented.

Boron is not considered to have endocrine disrupting effects. However, based on new regulations Commission Delegated Regulation (EU) No 2017/2100 for biocidal products and upcoming renewals for boron the assessments in terms of endocrine disrupting effects might be changed. Additionally, boron is classified with Toxic for reproduction category 1B with assigned risk phrase H360FD (see Commission Regulation (EU) 2018/669 of 16 April 2018). Therefore, boron should be considered as fulfilling the criteria for Persistence and Toxicity, but not for Bioaccumulation.

See Comparative assessment file.

Conclusion: Boron meets two of the criteria for being PBT in accordance with Annex XIII to Regulation (EC) No 1907/2006. As boric acid and disodium tetraborate fall within the scope of the Article 10(1)(a, d) of Regulation 528/2012 as a candidate for substitution, product can be authorised for a period of 5 years with comparative assessment according Article 23 of Regulation 528/2012.

## Measures to protect man, animals and the environment

Primary as well as secondary exposure of humans, non-target animals and the environment are minimised, by considering and applying the following appropriate and available risk mitigation measures:

- Authorisation is granted for Use Class 1 (wood or wood-based product under cover and fully protected from the weather, not exposed to wetting) and Use Class 2 (wood or wood-based product under cover and fully protected from the weather but where high environmental humidity can lead to occasional but not persistent wetting).

- Treated timber must not be permanently exposed to weather or used in external situations where it is in contact with the ground or in permanent contact with fresh or salt water.

- The preserved wood must be used only indoor or outdoor under cover and fully protected from the weather.

- Preserved wood must be protected from leaching until the roofing.

- Always read the label before use and follow the instructions provided.

- Avoid contact with skin and eyes.

- In case of contact with eyes, rinse immediately with plenty of water and seek medical advice.

- After contact with skin wash immediately with plenty of water.

- Avoid contact with clothing. Take off dirty cloth immediately.

- Contaminated gloves should be cleaned or disposed. Do not allow that water used for cleaning gloves get into the soil, surface water or sanitary sewer system.

- In the case of application by painting/brushing suitable personal protective equipment (coveralls, gloves, foot protection, eye protection glasses and respiratory protective equipment) are recommended when applying the product and when handling freshly treated timber. Avoid excessive contamination of protective equipment.

- In the case of application techniques as vacuum pressure impregnation, dipping and automated dipping suitable personal protective equipment (coveralls, gloves, foot protection, eye protection glasses and respiratory protective equipment) are required when applying the product and when handling freshly treated timber. Avoid excessive contamination of protective equipment.

- In case of accident (e.g. if swallowed) or if you feel unwell seek medical advice immediately (show packaging and the label).

- Wash hands and exposed skin before meals, drinking, smoking and after use.

- Do not mix with other products.

- The working area should be ventilated adequately by natural or mechanical means.

- Freshly treated wood should be stored in areas with good ventilation.

- The treated wood is not placed on the market until it is dry.

- Eating, drinking and smoking should be prohibited in areas where this product is handled, stored and processed.

- Do not use for wood in direct contact with food, feeding stuffs and drinking water.

- Biocidal product should not be used and stored where food, feeding stuffs or drinking water could be contaminated.

- Do not contaminate ground, waterbodies or watercourses with biocidal product or used container.

- Avoid release to the environment. Refer to special instructions/safety data sheet.

- Avoid contamination of soil, surface water or sanitary sewer system from product or packaging the product.

- In case of accidental release of product into the environment, it should be collected with non-combustible, absorbent material e.g. sand, earth, vermiculite and place in labeled and colder container for disposal and deliver to authorised company which is empowered to utilization of hazardous wastes and their disposal. During collect avoid direct contact with the skin.

- Do not empty into drains.

- If the product contaminates lakes, rivers, or sewers, inform the appropriate authorities in accordance with local regulations.

- Product contains substances potentially dangerous to bat.

- Product should be stored in original, labelled and closed containers in cool, dry and well-ventilated area.

- Keep in a safe place.

- Keep out of the reach of children.

- Containers that have been opened should be tightly closed and stored in vertical position.

- This material and its container must be disposed of in a safe way

- Packaging of the product, any contaminated materials (i.e. water used for cleaning of contaminated surface, protection foil, cleaning solvents), unused product, the remains of the product after use (closed in a labeled container) and the out-of-service treated wood must be treated as hazardous waste and delivered to authorised company which are empowered to utilization of hazardous wastes and their disposal.

- Package cannot be reused and be used for any other purpose.

- Application processes must be carried out within a contained area, situated on impermeable hard standing with bonding to prevent run-off and a recovery system in place (e.g. sump). Any leakages collect for reuse or recycling.

- Freshly treated timber must be stored after treatment under shelter and/or on impermeable hard standing with bonding and a recovery system in place (e.g. sump) to prevent direct losses to soil or water and that any losses must be collected for reuse or disposal.

# Proposal for decision

- Product Formulation

| Active substance content | % w/w | Manufacturer of active substance |
| --- | --- | --- |
| Boric acid | 15 | please referee to PAR section: Manufacturer of active substance used in the biocidal product |
| Disodium tetraborate | 5 |  |

| Formulation type | powder |
| --- | --- |
| Product type | PT8 |
| User | professional industrial |
| Packaging | please see to section 2.2.3 |
| Application | painting/brushing dipping vacuum pressure |
| Application Rate | superficial treatment 500 g/m2 of 20% working solution (100 g/m2 of concentrate) penetrating treatment 25 kg/m3 of 20% working solution (5 kg/m3 of concentrate). These doses are effective for prevention of against the wood rooting fungi and wood boring insects together |
| Organism controlled | Wood destroying basidiomycetes: Coniophora puteana, Gloeophyllum trabeum, Poria placenta Wood boring beetle: Hylotrupes bajulus, larvae |
| Shelf life | up to 2 years |
| Expiry data of the authorisation | 10 years after the date of authorisation granting |
| Any other specific conditions: | please see section 3.9. |

###### List of studies reviewed

List of new data submitted in support of the evaluation of the biocidal product

| Section No | Reference No | Author | Year | Title | Owner of data | Letter of Access | Data protection claimed |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | Yes | No | Yes | No |
| IIIB | 3.1.1 3.1.2 3.1.3 3.5 3.6 3.7 3.8 3.12 | Al Amin Idris | 2011 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. Determination of physicochemical properties. Institute of Industrial Organic Chemistry, Warsaw Report No. EMC Nr 373800019, Study code No. BF-25/11, | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB |  | Al Amin Idris | 2012 | Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. Determination of wettability. Institute of Industrial Organic Chemistry, Warsaw Report No. EMC Nr 333200019, Study code No. BF-25/11, | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 4.1 | Drożdżewska Katarzyna | 2011 | Badania analityczne “Przeciwogniowego Impregnatu do drewna FIRESTOP Koncentrat” Instytut Przemysłu Organicznego, Warszawa Report No EMC Nr 373800023 Study code No BA-12/11 | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 5.10-01 | Abram Alicja | 2011 | Wood Protector przeciwogniowy impregnat do drewna Firestop koncentrat Instytut Techniki Budowlanej, Warszawa, 2011 Test Report No LM 02-2265/10/Z00NM | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 5.10-02 | Abram Alicja | 2011 | Wood Protector przeciwogniowy impregnat do drewna Firestop koncentrat Instytut Techniki Budowlanej, Warszawa, 2011 Test Report No LM 01-2265/10/Z00NM | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| III-B | 5.10-03 | Fennert Eva-Maria, Doblinski M. | 2010 | Determination of the preventive action against recently hatched larvae of Hylotrupes bajulus (L.) according to EN 46-1 (2009) after evaporative ageing procedure according to EN 73 (1988). Wood Protector Firestop Koncentrat MPA Eberswalde, Test report No. 32/10/9443/02A | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| III-B | 5.10-04 | Fennert Eva-Maria, Doblinski M. | 2010 | Determination of the toxic values against recently hatched larvae of Hylotrupes bajulus (L.) according to EN 47 (06/2005) in combination with evaporative ageing procedure according to EN 73 (04/90) Wood Protector Firestop Koncentrat MPA Eberswalde, Test report No. 32/10/9443/03 | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 6.1.1 | Kupny Joanna, Fochtman Przemysław | 2011 | WOOD PROTECTOR przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. Acute oral toxicity study – fixed dose method on rats according to the OECD Guideline No 420/EU Method B.1.BIS. Institute of Industrial Organic Chemistry Branch Pszczyna, Study code: PO-8/11, | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 6.1.2 | Kupny Joanna, Fochtman Przemysław | 2011 | WOOD PROTECTOR przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. Acute dermal toxicity study on rats according to the OECD Guideline No 402/EU Method B.3. Institute of Industrial Organic Chemistry Branch Pszczyna Study code: DER-8/11 | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 6.2.1-1 | Gruszka Katarzyna, Fochtman Przemysław | 2011 | WOOD PROTECTOR przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. In vitro skin corrosion: Transcutaneous electrical resistance test (TER) according to the OECD Guideline No 430/EU Method B.40. Institute of Industrial Organic Chemistry Branch Pszczyna Study code:OES-4/11 | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 6.2.1-2 | Krupny Joanna, Fochtman Przemysław | 2011 | WOOD PROTECTOR przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. Acute skin irritation/corrosion study on rabbits according to the OECD Guideline No 404/EU Method B.4. Institute of Industrial Organic Chemistry Branch Pszczyna Study code: DDR-10/11, | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 6.2.2-1 | Gruszka Katarzyna, Fochtman Przemysław | 2011 | WOOD PROTECTOR przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. Isolated Chicken Eye Test Method for Identifying Ocular Corrosives and Severe Irritants according to the OECD Guideline No 438/EU Method B.48. Institute of Industrial Organic Chemistry Branch Pszczyna Study code: ICE-1/11 | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 6.2.2-2 | Kupny Joanna, Fochtman Przemysław | 2011 | WOOD PROTECTOR przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. Acute eye irritation/corrosion study on rabbits according to the OECD Guideline No 405/EU Method B.5. Institute of Industrial Organic Chemistry Branch Pszczyna Study code:ODR-12/11 | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |
| IIIB | 6.3 | Kupny Joanna, Fochtman Przemysław | 2012 | WOOD PROTECTOR przeciwogniowy impregnat do drewna FIRESTOP Koncentrat. Skin sensitization study according to the OECD Guideline No 406/EU Method B.6. Institute of Industrial Organic Chemistry Branch Pszczyna Study code:Al-7/11 | Dekspol P.P.H. Iwona Oleszak | ( | ( | ( | ( |

###### Analytical methods residues – active substance

< Boric acid >

< Disodium tetraborate >

No new data for the active substances residues was submitted. For datailed information please see the Competent Authority Reports for active substances boric acid and disodium tetraborate.

###### Toxicology and metabolism –active substance

< Boric acid >

< Disodium tetraborate >

No new data for the active substances was submitted. For datailed information please see the Competent Authority Reports for active substances boric acid and disodium tetraborate.

###### Toxicology – biocidal product

< Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat >

| General information |
| --- |
| Formulation Type: | powder |
| Active substance(s) (incl. content) | 15% boric acid, 5% disodium tetraborate |
| Category | PT 8 – wood preservatives |

| Acute toxicity, irritancy and skin sensitisation of the preparation (Annex IIIB, point 6.1, 6.2, 6.3) |
| --- |
| Rat LD50 oral (OECD 420) | > 2 000 mg/kg b.w |
| Rat LD50 dermal (OECD 402) | > 2 000 mg/kg b.w. |
| Rat LC50 inhalation (OECD 403) | - |
| Skin irritation (OECD 404) | Non irritat |
| Eye irritation (OECD 405) | Non irritat |
| Skin sensitisation (OECD 429; LLNA) | Non sensitiser |

| Additional toxicological information (e.g. Annex IIIB, point 6.5, 6.7) |
| --- |
| Short-term toxicity studies | Not required |  |  |  |
| Toxicological data on active substance(s) (not tested with the preparation) | For datailed information please see the Competent Authority Reports for active substances boric acid and disodium tetraborate. |
| Toxicological data on non-active substance(s) (not tested with the preparation) | The biocidal product contains one substance of concern – quaternary ammonium compounds, benzyl-C12-14-alkyldimethyl, chlorides (CAS 85409-22-9), trade name Barquat MS 100, classified and labeled under CLP regulation 1272/2008. The Barquat MS 100 concentration in the product is very low (0.66%) and does not affect on overall classification of product. Please see Doc.IIIB6.5 for details. |
| Further toxicological information | Not required |

| Classification and labelling proposed for the preparation with regard to toxicological properties (Annex IIIB, point 9) |
| --- |
| Directive 1999/45/EC | T- Toxic R60, R61 |
| Regulation EC 1272/2008 | Repr. 1B, H360FD |

###### Safety for professional operators

< Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat >

See point 2.7.3.1 above

###### Safety for non-professional operators and the general public

< Wood Protector przeciwogniowy impregnat do drewna FIRESTOP Koncentrat >

Biocidal product is intended to only to professional and industrial users.

###### Residue behaviour

< Boric acid >

< Disodium tetraborate >

No new data for the active substances was submitted. For datailed information please see the Competent Authority Reports for active substances boric acid and disodium tetraborate.

###### Confidential information – ONLY FOR RMS INFORMATION, NOT FOR APPLICANT

This part of the Product Assessment Report contains data submitted NOT by applicant.

Applicant did not submitted the access for certain value which was used in the calculation by Polish Competent Authority, therefore information contained in this Annex are NOT intended for the applicant but for the Member States only.

# Footnotes

According to EN 335-1:2006, Durability of wood and wood-based products. Definition of use classes. Part 1:General

Competent Authority Reports available at https://circabc.europa.eu

Technical Notes for Guidance (TNsG). Human Exposure to Biocidal Products – Guidance on Exposure Estimation. Contract B4-3040/2000/291079/MAR/E2. DG Environment June 2002.User Guidance, Version 1 belonging to Report Human Exposure to Biocidal Products (TNsG June 2002). Available from http://ecb.jrc.it

Emission Scenario Documents, number 2, Emission Scenario Document for Wood Preservatives, Part I OECD 2003

According to HEEG opinion 18, Default human factor values for use in exposure assessments for biocidal products

Commission Directive 2009/94/EC

Commission Directive 2009/91/EC

Technical Guidance Documents on Risk Assessments